## Slide 1
Start: specify the specimen and total loads Qmax, Qmin
Locate actual crack–reinforcement intersections
Initialize N=0, local counts Ni=0 and slip/failure history
parameters / prepare_parameters / fatigue_calculate
Solve initial peak and valley shear equilibrium in order
Vc(q)+Vs(q)+Vf(q)=Qmax/2 or Qmin/2
state → trial; internal calculation on page 2
Initial peak and valley
solutions successful?
N < Nmax?
Identify active nodes from peak–valley slip
(smax>0.75δm or previously activated) AND slip range>tol
active_nodes | F: threshold; history/range gates: code rules
Active nodes, or enabled
steel/concrete S–N rules?
Choose ΔN without passing the next snapshot or Nmax
Propose Ni,new=Ni,old+ΔN at active nodes only
Keep the accepted history unchanged until acceptance
Update nodal peak bond stress [F, Eq. 2]
τm,i=max{0,[1−kf log₁₀max(Ni,1)]τm,0}
kf=0.1965 (rod) or 0.1985 (strip) | bond_strength
Use the updated bond law to solve peak equilibrium
Crack jump q → slip profiles → bar forces → shear
state → trial → anchorage / bond (page 2)
Peak failed or q grew too fast,
AND ΔN > 1?
Candidate peak
equilibrium successful?
Use peak maximum-slip history to solve the valley state
FRP bond stress = historical secant stiffness × current slip
state → trial; valley shear target Qmin/2
Candidate valley
equilibrium successful?
Accept the block: N←N+ΔN; commit candidate history
Save q, w, v, Vc, Vs, Vf and local slip/strain/failure fields
fatigue_calculate / save_snapshot
Stop and export the last accepted response
export_results; reaching Nmax is a runout, not fatigue life
Reduce the cycle block
ΔN←max[1,floor(ΔN/2)]
Retry from the same accepted history
Record the stopping reason
Numerical failure / user limit /
no root on the selected branch
Do not label every stop as debonding
Cycle limit reached
Report runout
No active degradation mechanism
Record snapshots up to Nmax
Report runout without degradation
Yes: save N=0
No
Yes
No
Yes
No
Yes
No
Yes
No
Yes
No
Next block
Formula-Mapped Shear Fatigue Main Loop
F: 2019 flexural-fatigue modeling paper; S: 2019 single-crack shear paper; E: 2024 ECC-FRP paper. Equation numbers need a paper prefix.

## Slide 2
Set the peak/valley target and accepted history; trial q
state: ascending-bracket scan and bisection; no trial commit
1. Crack kinematics (prescribed code relations)
g(y)=(1−y/hc)^m; K=cosθ+r sinθ
w₀=q/K; v₀=rw₀; w(y)=w₀g(y); v(y)=v₀g(y)
crack_deformation | S, Eq. 7 (PST/Green) not implemented
2. Concrete shear (empirical code closure)
Vc=Vc0(1−exp(−q/qr))
×[ρc+(1−ρc)exp(−w₀/wc)](1−Dc)
trial | empirical parameters require calibration
3. Contribution of stirrups intersecting the crack
εs,j=qg(yj)/ls; σs,j=min(Esεs,j,fy); Vs=ΣAs,jσs,j
ls is assumed; stirrup stress is zero when damage reaches 1
trial | stress cap/sum: R22, Eqs. 9a, 9c
4. Project crack motion onto each intact FRP bar
δj=qg(yj)[sin(θ+αj)−r cos(θ+αj)]/K
For vertical bars (αj=90°): δj=qg(yj)
trial | not a direct substitution of S, Eq. 8
5. Update τm,i using local cycle counts [F, Eq. 2]
τm,i=max{0,τm,0[1−kf log₁₀max(Ni,1)]}
bond_strength; Ni counts local cycles after activation
6. Trilinear bond envelope [F, Eq. 1]; tr=min(τr,τm,i)
τenv=τm,i·s/δm s≤δm
τenv=tr+(τm,i−tr)(δu−s)/(δu−δm) δm<s≤δu
τenv=tr s>δu
bond | residual clipping and secant history: code additions
7. Discretize both anchors and integrate bond stress
dT/dx=−pfτ; ds/dx=−T/(EfAf); free-end T=0
Ti(x)=pf∫[x,Li]τi(ξ)dξ | anchorage / anchor_mesh
F, Eq. 10; S, Eq. 10: adapted to local anchor coordinates
8. Enforce two-sided compatibility and strain continuity
s₁(0)+s₂(0)=δj [S, Eq. 9d]; εf1(0)=εf2(0) [S, Eq. 11]
The same EfAf on both sides gives T₁(0)=T₂(0)
Numerical iteration; not F, Eq. 9b or S, Eqs. 9a–c
9. Check debonding, tensile and user cover limits
Remove failed-bar force; repeat steps 4–9 for other bars
trial: tensile cap Af·ffu; no FRP material-fatigue law yet
10. Sum FRP vertical forces and total shear
Vf=nfaces ΣTj sinαj; V=Vc+Vs+Vf=Q/2
Same force-decomposition idea as E, Eq. 1; Vf is NSM shear
The ECC-overlay split Vef,σ+Vef,τ is not used
Valid local solution AND
|V(q)−Q/2|≤forceTolerance?
Return the balanced peak/valley state and local fields
The controller decides whether to accept the cycle block
Further scan/bisection
search available?
Return a classified diagnostic
No selected-branch root /
numerical failure / resolution limit
No automatic IC-debonding label
Yes
No
Yes: adjust q
No
Formula-Mapped Shear Equilibrium Solver
F: DOI 10.1016/j.ijfatigue.2019.04.039; S: DOI suffix 0000953; E: CCENG-4395. Orange boxes include model assumptions.

## Slide 3
How the supplied equations relate to the current shear code
Adopted: F, Eq. (1), trilinear envelope; F, Eq. (2), local fatigue degradation
bond.m / bond_strength.m; the 0.75δm threshold is used in active_nodes.m
The code adds zero-count protection, nonnegative peaks and a residual-stress rule.
Adapted principle: bond-stress integration in F, Eq. (10), and S, Eq. (10)
Replace half-span coordinates with local coordinates on each anchor: Ti(x)=pf∫[x,Li]τi dξ
S, Eqs. (9d) and (11), motivate two-sided slip compatibility and intersection strain continuity.
Not directly implemented: F, Eq. (9b), analytical matrix; S, Eqs. (9a–c), analytical slip fields
anchorage.m assembles bar/bond stiffness and uses fixed-point iteration with a Newton fallback.
The numerical system is not the paper matrix merely because both are written as matrix equations.
Not included: Ps/Pd from F, Eq. (11), and half-span Ls/Ld relations from F, Eq. (13)
These belong to the longitudinal flexural IC-debonding model; its P is not this model’s total load Q.
The current code does not calculate critical loads or half-span damage-zone lengths using these equations.
Not included: longitudinally strengthened beam deflection from F, Eq. (14)
The eccentric longitudinal-reinforcement bending expression does not transfer directly to vertical NSM shear.
Here q is a vertical crack jump and w is crack opening; the paper’s deflection w is a different quantity.
Adopted equilibrium idea: E, Eq. (1), V=Vc+Vs+Vef
Here V=Vc+Vs+Vf, where Vf sums the actual NSM bar-force vertical components.
E, Eq. (2), Vef,σ+Vef,τ, concerns the continuous ECC overlay and is not implemented for these NSM bars.
This diagram describes the current calculation; the MATLAB source remains unchanged.
Implementing F, Eqs. (9b), (11), (13), or the complete S crack model requires separate modeling and validation.
Equations not yet implemented are not presented as executed calculation steps.
Equation Scope and Current Implementation
R22: DOI suffix 0001251, intersecting reinforcement and shear-force decomposition. This update translates the diagrams only.